1. Compliance and classification

The proposed sports flooring system must comply with the EN 14904 standard for indoor sports surfaces and be classified as Type A4, offering area-elastic performance characteristics.

2. System description

The flooring system shall be an area-elastic construction, consisting of a PVC surface layer fully adhered to a sub construction of birch plywood over a resilient foam underlayer.

- Total system thickness: Minimum 32 mm

- System components:

  - Polyethylene film 200µ thick as moisture barrier

  - PU foam underlayer, 15 mm thick, density 60 kg/m³, supplied in rolls of 1.6 m x 25 m

  - Birch plywood board, 15 mm thick, 100% birch composition, with double tongue & groove interlocking system. Board dimensions: 2490 mm x 395 mm

  - PVC compact top layer, 2 mm thick, supplied in rolls of 2 m width and 23 linear meters in length

3. Sports performance characteristics

The flooring system must deliver high-performance properties in accordance with the relevant EN standards for indoor sports surfaces:

- Shock Absorption (EN 14808): minimum 55% Type A4

- Vertical Deformation (EN 14809): between 2.3 and 5mm Type A4

- Ball Rebound (EN 12235): above 95%

- Friction (EN 13036-4): between 80 and 110 to ensure optimal grip and player safety

- Wear Resistance (EN ISO 5470-1, Taber test): below 100 mg

- Residual Indentation (EN 1516): below 0.1 mm

4. Fire classification

The complete flooring system must achieve at least Cfl-s1 classification in accordance with EN 13501-1 fire resistance standards.

5. Surface layer – PVC (Vinyl)

The PVC (vinyl) surface must meet the following environmental and technical criteria:

- Construction & surface treatment

  - The vinyl floor covering shall be reinforced with a non-woven fiberglass mat to ensure dimensional stability and mechanical strength.

  - The wear layer must be treated with Top Clean XP™, a UV photo-crosslinked polyurethane surface treatment applied in factory, providing enhanced resistance to abrasion, scuffing, and easy maintenance.

  - The product must offer a consistent top embossing across solid, wood and concrete designs, ensuring uniform appearance and performance regardless of design choice.

- Certifications & health labels

  - Must carry the Allergy UK Seal of Approval, attesting to its suitability for allergy-sensitive environments.

- Composition

  - Contains a minimum of 32% recycled content.

  - The formulation must be phthalate-free, including recycled content, and biocide-free, reducing exposure to potentially harmful substances.

- Indoor Air Quality & Emissions

- VOC emissions must be tested in accordance with EN 16516, after 28 days.

- TVOC, TSVOC, and formaldehyde emissions must be below 10 µg/m³, near the quantification limit, ensuring extremely low emissions and optimal indoor air quality.

- Circularity & Recyclability

- The product must be 100% recyclable.

- Clean off-cuts generated during installation must be eligible for collection and reintegration into the production cycle through the Restart® program or an equivalent circular economy initiative.

6. Environmental and health compliance

The complete system must comply with REACH regulations regarding the use of hazardous substances.

Use of low-emission, non-toxic components is mandatory to ensure safe indoor air quality and environmental protection.

7. Warranty

The product shall carry a minimum warranty of 15 years, covering material under standard use and maintenance conditions.

8. Installation requirements

- Subfloor preparation: A preliminary slab check is required. Surface irregularities must not exceed 6 mm under a 3 m straightedge.

- Temperature conditions: Installation should occur only when ambient conditions meet the manufacturer’s recommended temperature range.

- Installation method: Must follow both manufacturer’s guidelines and local regulatory standards to ensure optimal performance and durability.

Available documentation & certificates

- Technical datasheet

- Multi-language DoP (Declaration of Performance)

- EN 14904 certificate of compliance

- Reaction to fire test report

- VOC emissions report

- Allergy UK Seal of Approval for Omnisports

- Installation and maintenance guides

Contact us

For any additional information, Tarkett Sports experts remain at your disposal to assist you throughout your project.

info.tarkettsports.indoor@tarkett.com
 eu.tarkettsportsindoor.com