1. Compliance and classification

The proposed sports flooring system must comply with the EN 14904 standard for indoor sports surfaces and be classified as Type C4, offering combined-elastic performance characteristics.

2. System description

The flooring system shall be a combined construction, consisting of a PVC surface layer fully adhered to a sub construction of birch plywood over a resilient foam underlayer.

- Total system thickness: Minimum 36.3 mm

- System components:

  - Polyethylene film 200µ thick as moisture barrier

  - PU foam underlayer, 15 mm thick, density 60 kg/m³, supplied in rolls of 1.6 m x 25 m

  - Birch plywood board, 15 mm thick, 100% birch composition, with double tongue & groove interlocking system. Board dimensions: 2490 mm x 395 mm

  - PVC P1 Type top layer, 6.2 mm thick, supplied in rolls of 2 m width and 20.5 linear meters in length

3. Sports performance characteristics

The flooring system must deliver high-performance properties in accordance with the relevant EN standards for indoor sports surfaces:

- Shock Absorption (EN 14808): minimum 60% Type C4

- Vertical Deformation (EN 14809): between 2.3 and 5mm Type C4

- Ball Rebound (EN 12235): above 95%

- Friction (EN 13036-4): between 80 and 110 to ensure optimal grip and player safety

- Wear Resistance (EN ISO 5470-1, Taber test): below 250 mg

- Residual Indentation (EN 1516): below 0.2 mm

4. Fire classification

The complete flooring system must achieve at least Cfl-s1 classification in accordance with EN 13501-1 fire resistance standards.

5. Surface layer – PVC (Vinyl)

The PVC (vinyl) surface must meet the following environmental and technical criteria:

- Construction & surface treatment

  - The vinyl floor covering shall be reinforced with a non-woven fiberglass mat to ensure dimensional stability and mechanical strength.

  - The wear layer must be treated with Top Clean XP™, a UV photo-crosslinked polyurethane surface treatment applied in factory, providing enhanced resistance to abrasion, scuffing, and easy maintenance.

  - The product must offer a consistent top embossing across solid, wood and concrete designs, ensuring uniform appearance and performance regardless of design choice.

- Certifications & health labels

  - Must carry the Allergy UK Seal of Approval, attesting to its suitability for allergy-sensitive environments.

- Composition

  - Contains a minimum of 21% recycled content.

  - The formulation must be phthalate-free, including recycled content, and biocide-free, reducing exposure to potentially harmful substances.

- Indoor Air Quality & Emissions

- VOC emissions must be tested in accordance with EN 16516, after 28 days.

- TVOC, TSVOC, and formaldehyde emissions must be below 10 µg/m³, near the quantification limit, ensuring extremely low emissions and optimal indoor air quality.

- Circularity & Recyclability

- The product must be 100% recyclable.

- Clean off-cuts generated during installation must be eligible for collection and reintegration into the production cycle through the Restart® program or an equivalent circular economy initiative.

6. Environmental and health compliance

The complete system must comply with REACH regulations regarding the use of hazardous substances.

Use of low-emission, non-toxic components is mandatory to ensure safe indoor air quality and environmental protection.

7. Warranty

The product shall carry a minimum warranty of 15 years, covering material under standard use and maintenance conditions.

8. Installation requirements

- Subfloor preparation: A preliminary slab check is required. Surface irregularities must not exceed 6 mm under a 3 m straightedge.

- Temperature conditions: Installation should occur only when ambient conditions meet the manufacturer’s recommended temperature range.

- Installation method: Must follow both manufacturer’s guidelines and local regulatory standards to ensure optimal performance and durability.

9. Sport federation approvals

The flooring system should be recommended or certified by international sports federations, including:

- FIBA (Basketball)

- IHF (Handball)

Available documentation & certificates

- Technical datasheet

- Multi-language DoP (Declaration of Performance)

- EN 14904 certificate of compliance

- Reaction to fire test report

- VOC emissions report

- Allergy UK Seal of Approval for Omnisports

- Installation and maintenance guides

- FIBA and IHF certification

Contact us

For any additional information, Tarkett Sports experts remain at your disposal to assist you throughout your project.

info.tarkettsports.indoor@tarkett.com
 eu.tarkettsportsindoor.com