1. Compliance and classification

The proposed sports flooring system must comply with the EN 14904 standard for indoor sports surfaces and be classified as Type A4, offering area-elastic performance characteristics.

2. System description

The flooring system shall be an area-elastic construction, consisting of a linoleum surface layer fully adhered to a sub construction of birch plywood over a resilient foam underlayer.

- Total system thickness: Minimum 41.2 mm

- System components:

  - Polyethylene film 200µ thick as moisture barrier

  - PU foam underlayer, 20 mm thick, density 80 kg/m³, supplied in tiles of 2 m x 1 m

  - Birch plywood panel, 18 mm thick, 100% birch composition, with tongue & groove interlocking system. Panel dimensions: 2400 mm x 1200 mm

  - Linoleum top layer, 3.2 mm thick, supplied in rolls of 2 m width and approximately 28 linear meters in length

3. Sports performance characteristics

The flooring system must deliver high-performance properties in accordance with the relevant EN standards for indoor sports surfaces:

- Shock Absorption (EN 14808): minimum 55% Type A4

- Vertical Deformation (EN 14809): between 2.3 and 5mm Type A4

- Ball Rebound (EN 12235): above 90%

- Friction (EN 13036-4): between 80 and 110 to ensure optimal grip and player safety

- Wear Resistance (EN ISO 5470-1, Taber test): below 1g

- Residual Indentation (EN 1516): below 0.2 mm

4. Fire classification

The complete flooring system must achieve at least Cfl-s1 classification in accordance with EN 13501-1 fire resistance standards.

5. Surface layer – Linoleum

The linoleum surface must meet the following environmental and health criteria:

- Cradle to Cradle Certified® Silver

- Allergy UK Seal of Approval

- Composition:

  - Minimum 93% natural raw materials

  - At least 39% recycled content

  - 76% biobased

- Emissions:

  - VOC emissions tested according to EN 16516 after 28 days

  - TVOC, TSVOC and formaldehyde emissions must be below 10 µg/m³, close to the quantification limit

- 100% recyclable, with clean off-cuts and post-use material eligible for collection and reintegration via the Restart® program or equivalent circular economy initiatives

6. Environmental and health compliance

The complete system must comply with REACH regulations regarding the use of hazardous substances.

Use of low-emission, non-toxic components is mandatory to ensure safe indoor air quality and environmental protection.

7. Warranty

The product shall carry a minimum warranty of 10 years, covering material under standard use and maintenance conditions.

8. Installation requirements

- Subfloor preparation: A preliminary slab check is required. Surface irregularities must not exceed 6 mm under a 3 m straightedge.

- Temperature conditions: Installation should occur only when ambient conditions meet the manufacturer’s recommended temperature range.

- Installation method: Must follow both manufacturer’s guidelines and local regulatory standards to ensure optimal performance and durability.

Available documentation & certificates

- Technical datasheet

- Multi-language DoP (Declaration of Performance)

- EN 14904 certificate of compliance

- Reaction to fire test report

- VOC emissions report

- Allergy UK Seal of Approval / Cradle to cradle certificate for Linosport xf²

- Installation and maintenance guides

Contact us

For any additional information, Tarkett Sports experts remain at your disposal to assist you throughout your project.

info.tarkettsports.indoor@tarkett.com
 eu.tarkettsportsindoor.com