AQUA MULTISAFE

Product Description

13/09/2024

Aqua Multisafe collection is part of the Wetroom concept (Aquasens) and can be combined with the wall covering Aquarelle HFS and with the wetroom accessories.

Aqua Multisafe belongs to the norm ISO 10582, Heterogeneous vinyl compact floor covering in roll format, available in 2m width. It has a 2mm total thickness with a wear layer of 0.55mm. Its fire resistance is rated Bfl-s1 under the norm EN13501-1. The collection contains 10 references with designs certified by Dementia Service Development Centre (DSDC).

The product has an optimized embossing to ensure the best barefoot anti-slip resistance (rated class C under the norm DIN EN 16165 NB 1) and an excellent shod anti-slip resistance (rated R10 classification under the norm DIN EN 16165 NB2).

It has to be fully glued and hot welded for optimal hygiene and perfect watertightness, offering a seam strength > 240N/50mm under the EN 16906 standard. It is resistant to stains and chemicals. Bacteria resistance is measured as “does not promote growth” following the requirement of ISO 846 part C.

The product formulation is free of phthalates and biocides. It contains 33% recycled material. The installation offcuts could be recyclable and collected through the ReStart® take-back recycling program (contact your Tarkett sales representative). The product benefits from an Environmental Product Declaration (EPD).

The TVOC and formaldehyde emissions will be below 10 μg/m³ based on the EN 16516 standard. Aqua Multisafe is produced in France & comes with a 10 Year Warranty.

Documents available on our website

Technical Data sheet / Green building card / lnstallation Guide / Maintenance Guide / EPD / DOP / Warranty

Plant certifications

ISO 14001:2015 - Environmental management systems

ISO 50001:2018 - Energy management systems

ISO 9001:2015 - Quality management systems

ISO 45001:2018 - Occupational health and safety management systems

Commercial launch date October 2024. Information can be modified (Edition 09/2024).