AQUARELLE HFS

Product Description

12/09/2024

Aquarelle HFS collection is part of the Wetroom concept (Aquasens) and can be combined with one of these anti-slip floors Aqua Multisafe, Granit Multisafe, Granit Safe T and with the wetroom accessories.

Aquarelle HFS belongs to the norm EN 233, Heterogeneous vinyl compact wall covering in roll format, available in 2m width and in 49cm width for the Aquarelle HFS border. It has a 0.92mm total thickness with a wear layer of 0.12mm. Its fire resistance is rated B-s2 d0 under the norm EN13501-1. The collection contains 32 references with designs certified by Dementia Service Development Centre (DSDC).

The product is flexible to ease the installation, it has to be fully glued and hot welded for optimal hygiene and perfect watertightness, offering a seam strength > 150N/50mm under the EN 16906 standard. It is resistant to stains and chemicals, it has an excellent cleanability based on the riboflavin cleanability test (Fraunhofer test method report). Bacteria resistance is measured as “does not promote growth” following the requirement of ISO 846 part C.

The product formulation is free of phthalates and biocides. It contains 4.5% recycled material. The installation offcuts could be recyclable and collected through the ReStart® take-back recycling program (contact your Tarkett sales representative). The product benefits from an Environmental Product Declaration (EPD).

The TVOC and formaldehyde emissions will be below 10 μg/m³ based on the EN 16516 standard. Aquarelle HFS is produced in Luxembourg & comes with a 10 Year Warranty.

Documents available on our website

Technical Data sheet / Green building card / lnstallation Guide / Maintenance Guide / EPD / DOP / Warranty

Plant certifications

ISO 14001:2015 - Environmental management systems

ISO 50001:2018 - Energy management systems

ISO 9001:2015 - Quality management systems

ISO 45001:2018 - Occupational health and safety management systems

Commercial launch date October 2024. Information can be modified (Edition 09/2024).