Product Description

Granit Safe.T

9/19/2024

Granit Safe.T belongs to the category of polyvinyl chloride floor coverings with particle based enhanced slip resistance according to EN standard 13845, use class 34/43. It has a 2,0 mm thickness with a wear layer thickness of 2,0 mm and is available in 2 m wide sheets. It is produced in a subtle directional pattern with a weight of 2950 g/sqm. It has a slip resistance of R10 accoridng to DIN 51130, a slip resistance class C according to DIN 51097. It is approved for wetroom installation according to EN 13553 Annex A with a watertight rating. The fire resistance of the product is rated Bfl-s1.

The product offer an "Good Resistance" ranking to chemical stain resistance based on the ISO 26987 standard being resistant to disinfectants and antiseptics used in healthcare settings and a bacteria resistance of "Does not promote growth" following the requirement of ISO 846 part C.

This product is flexible enough to allow coving up against the wall if requested in order to ease cleaning and maintenance operations and can be heat welded for optimal watertightness. Welding rods are available in uni and multicolour options, a colour and pattern-coordinated welding rod, so the look will always be seamless. Granit Safe.T comes with a 10 year warranty.

The product formulation is free of phthalates and biocides. It contains an average of 25% recycled material. The installation offcuts and post-consumer material must be recyclable in accordance with ISO 14021, meaning that the offcuts and post-consumer (after usage) material can be collected through the ReStart®  take-back recycling program. Upon request, Tarkett is able to issue a certificate showing the carbon savings due to the take back and recycling program. The product benefits from an Environmental Product Declaration (EPD) and from a third party verified Material Health Statement (MHS) with evaluation threshold of 0,01%. TVOC after 28 days will not exceed 10µg/m3 based on the EN 16516 standard. The material contributes to sustainable building labels LEED, BREAM, and WELL, among others.

Available documents on our website

Technical Data sheet / Green building card / Installation Guide / Maintenance Guide / Fire report / EPD / MHS / DOP / Warranty

Plant certifications

ISO 14001:2015 - Environmental management systems

ISO 50001:2018 - Energy management systems

ISO 9001:2015 - Quality management systems

ISO 45001:2018 - Occupational health and safety management systems