Product Description

iQ Optima

17/05/24

iQ Optima belongs to the category of Homogeneous poly(vinyl chloride) floor covering according to ISO standard 15081, use class 34/43, with a binder content Type I. It has a 2mm thickness with a wear layer thickness of 2mm and is available in 2m wide sheet and 61x61 tiles and is produced in a directional pattern with translucent chips. With a weight of 2650g/m² its best indentation resistance value will be 0.02mm, and has a slip resistance of R9. Fire resistance is rated Bfl-s1.

The product is antistatic ≤2kV (EN 1815), and offer an "Excellent Resistance" ranking to chemical stains resistance based on the ISO 26987 standard. It is also granted with an "Excellent" cleanability result (Fraunhofer method test report), and a bacteria resistance of "Does not promote growth" following the requirement of ISO 846 part C. The product can be installed in the most demanding environments such as ISO 4 cleanrooms (ISO14644-1). iQ Optima is available in compact and acoustic versions. The acoustic version increases underfoot comfort and reduces sound transmission by 16dB (EN ISO 717-2).

This product is flexible enough to allow coving up against the wall if requested in order to ease maintenance operations, and be heat welded for optimal watertightness. Welding rods (multicolour and unicolour) are available in matching colours coordinated with flooring pattern designs to ensure a perfect finish. A selection of 10 colours are tested and accredited Dementia Services Development Centre (DSDC) with 1b, suitable for dementia friendly designing. iQ Optima enables dry buffing to restore the surface without any need of chemicals and is also easily repairable avoiding replacement when the surface is damaged.

The product formulation is free of phthalates and biocides. It contains on average over 25% recycled material. The installation offcuts and post-consumer material must be recyclable in accordance with ISO 14021, meaning that the offcuts and post-consumer (after usage) material can be collected through the ReStart® a take-back recycling program. Upon request, Tarkett is able to issue a certificate showing the carbon savings due to the take back and recycling program. The product benefits from an Environmental Product Declaration (EPD) and from a third party verified Material Health Statement (MHS) with evaluation threshold of 0.01%. TVOC after 28 days will not exceed 10µg/m3 based on the EN 16516 standard. The material contributes to sustainable building labels LEED, BREAM, and WELL, among others.

Available documents on our website

Technical Data sheet / Green building card / Installation Guide / Maintenance Guide / Fire report / EPD / MHS / DOP / Warranty

Plant certifications

ISO 14001:2015 - Environmental management systems

ISO 50001:2018 - Energy management systems

ISO 9001:2015 - Quality management systems

ISO 45001:2018 - Occupational health and safety management systems